## Slide 1: Composites for Beginners
Tony Tao
2022.10.06
16.82x

## Slide 2: Composite Materials
Matrix (Epoxy or other thermoset plastic)
Fibers (Carbon fiber, Kevlar, fiberglass…)
Engineered composite material a material consisting of two or more materials which - when combined - generates properties superior to the properties of the proportional average of the materials
Other examples:

## Slide 3: Advantages of Composites vs Metals
Composites
Smooth, complex 3D curves
Non-isotropic tailoring
Cost-insensitive, weight-critical
Metals
Fastening
High temperatures
High surface-speed rubbing
Suitability
F1 rear wing
Car knuckle
Ball bearings
Aerospace primary structure

## Slide 4: Fiber Organization
“Unidirectional fabric”
“Tow” or “Yarn”
“Woven fabric”
Fiber “strand”
Human hair
50-30%
50-70%
By mass

## Slide 5: Fiber and Fabric Jargon
Tow
Fiber count/bundle
  1000 = “1K”
  3000 = “3K”
Woven Fabric
Weave
Weight
  6 oz/yd2
  200 gsm (g/m2)
Tow size
Bias
Thickness
Fibers
UHM = “ultra high modulus” very stiff & brittle
HM = “high modulus” stiff & brittle
IM = “intermediate modulus” strongest
SM = “standard modulus” springy, cheapest
Uni fabric
= woven fabric +…
Binding
  Net 
  Stitching 
  Web 
P.S.: Cost is non-monotonic with weight!

## Slide 6: Fiberglass
Most compliant
Most economical
Many moduli available (E, S, etc)
Available in lightest weights
Commonly-available fabric weights:
  0.6, 0.7, 1.4, etc etc
  0.6, 0.7 considered “finishing glass”
Limiting single-layer dry weight: ~0.6 oz

## Slide 7: Kevlar (Aramid)
High tensile strength
Poor compressive strength
UV-sensitive
Annoying to work with (difficult to cut cleanly)
Commonly-available fabric weights:
  1.0, 1.7, 5.0
Limiting single-layer dry weight: ~1.7 oz
Many UAV shells are made from Kevlar – why?
Protip: Heat prior to wet layup to remove moisture

## Slide 8: Carbon Fiber
High Modulus (both compressive and tensile)
High UTS
High cost
Can be brittle, depending on fiber selected
Commonly-available fabric weights:
  2.4, 3.5, 5.7, 10.9
Limiting single-layer dry weight: ~2.5 oz

## Slide 9: Common fiber material summary table
 | Carbon Fiber | Fiberglass | Aramid (Kevlar)
Tensile str | Excellent | Good | Excellent
Compression str | Excellent | Good | Terrible
Spring energy | Good | Excellent | Bad
RF penetration | Bad | Good | Good
Abrasion resist. | Bad | Bad | Good
Processing | Okay | Okay | Terrible
Price | High | Low | Med
Density | High | Low | Low

## Slide 10: Weaves and Multi-Species Fabrics
Plain Weave
Carbon-Kevlar hybrid
Twill Weave
Good at conforming to 3D shapes
Somewhat difficult to handle
Carbon-metal hybrid
Honeycomb Weave
4HS Satin Weave
Easiest to work with for flat shapes
Easiest to handle
Looks neat ???
Conforms to holes, 3D shapes
Difficult to handle

## Slide 11: Composite Manufacturing Process
“Carbon Fiber Reinforced Polymer (…) fabrication has been described as a black art. What is it, really?”
http://www.mmsonline.com/articles/getting-to-know-black-aluminum
≈
Answer:

## Slide 12: Molds
Molds may be metal, composite, plastic, whatever
May be solid or compliant (silicone, etc)
Release agents must be used for most molds
Molds are often painted before layup; paint will stay with composite part 

## Slide 13: Lay-up Process Basics
Mold
Release agent (spray, wipe, or wax)
Epoxy
Butyl tape
Fabric (wet)
Foam core
Porous release film
(or peel ply)
Breather
Bagging film

## Slide 14: Lay-up Process Basics
Work time for epoxy ~a few hours
Cure time ~18-24 hours before debagging (faster with heat, but plastics and mold may not survive)
Debagging can break parts, be careful
Mold
Mold
Under Vacuum Compression:
Before Compression:
Air bubbles
Carbon fibers
Epoxy
Purpose of vacuum:
Remove air bubbles
Reduce inter-fiber distance

## Slide 15: Technique: Wet lay-ups
Fibers are wetted with epoxy
Bagged onto mold while wet (with excess)
Excess epoxy is absorbed or bled out
(+) Minimal equipment
(+) Can achieve very low weight
(-) …but is less reliable at it
(-) Fairly labor-intensive

## Slide 16: Technique: Resin Infusion
Fibers are placed in mold dry
Vacuum-bagged while dry
Resin from reservoir is pulled in by vacuum pressure
(+) Less labor than wet layup
(-) Epoxy viscosity critical
(-) More wasteful (epoxy, plumbing)
(-) Can’t achieve as low a weight as wet layup

## Slide 17: Technique: Pre-preg
Fibers pre-impregnated with high temperature epoxy
Fabrics are assembled, bagged, and cured under pressure + heat
(+) Cleanest
(+) Maximum strength
  High pressure fiber packing, better microstructure of impregnated epoxy
(+) Low labor cost
(-) Very high equipment cost (freezer, autoclave)
(-) Prepreg has expiration date due to pre-mix

## Slide 18: Fillers
Used to change properties of epoxy (viscoelasticity, density, strength)
Can lighten bulky regions
  Microballoons (don’t breathe these)
Can strengthen
  Colloidal silica (don’t breathe these either)
  Chopped fiber (nope, not these guys either)

## Slide 19: Mass and Strength Estimation
Laminates are orthotropic
Material strength depends on load direction
Strength: Longitudinal/transverse 10/1
Multiple layers can be stacked to build “quasi-isotropic” material
Longitudinal
Transverse

## Slide 20: Typical Design First-Estimates
Spar: 0°
D-tube: 45°-45°
0°
90°
Euler beam bending
Unidirectional modulus & strength
Closed section torsion
45-45 laminate direction
Beware of out-of-plane buckling constraint